PT.Bumi Laut Perkasa

Jl.Brigjen Katamso Km 06 Tanjung Uncang – Batam

AWS D1.1 Welding Procedure Specification (WPS)

| WPS Record No | : | BLP/WPS/VI/08/Rev03 |  | Issue Date | : | June 24 ,2008 |
| --- | --- | --- | --- | --- | --- | --- |
| Supporting PQR.No. (s) | : | - |  | Prequalified | : | Yes No |
| Welding Process | : | SMAW |  | Type | : | Manual |
| Welding Position | : | 3G |  | Welding Progression | : | (Uphill) (Downhill) |

| Joint Design |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| AWS Joint Designation | : | B – U2 |  | Type | : | Butt ( Single V Groove) |
| Back Gouging | : | Yes No |  | Backing Material | : | Yes No |
| Reference code | : | AWS D1.1 |  |  |  |  |

Welding Sequence

| Base Materials Details |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Specification and Grade – Side 1 | : | ASTM A283 Grade C |  |  |  |  |
| Specification and Grade – Side 2 | : | ASTM A283 Grade C |  |  |  |  |
| Form |  | Thickness Range (mm) | : | 5 to 25 mm |  | Pipe Outside Dia (mm): |
| Plate |  |  |  |  |  |  |

| Consumable Details |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Filler Metal | : | AWS A 5.1 E6013 |  |  |  |  |  |  |  |  |
| Name | : | Golden Bridge E4313 |  |  |  | GB Model | : | J421 |  |  |
| Filler Metals Sizes (mm) | : | Ø 3.2 |  |  |  |  |  |  |  |  |
| Gas Composition | : | Shielding | : | N/A |  | Gas Flow Rate | : | Shielding | : | N/A |
|  |  | Backing | : | N/A |  |  |  | Backing | : | N/A |
| Tungsten Electrode Type & Size | : | N/A |  |  |  |  |  |  |  |  |

| Preheat/Heat Treatment Details : |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Pre Heat Temperature °C (min) | : | 150° C |  | Interpass Temperature °C (max) | : | 225° C |
| Post Weld Heat Treatment and/or ageing |  |  |  | Temperature: 550° C Time | : | 2 Hours |
| Method |  |  |  |  |  |  |
| Heating and Cooling Range 100 – 130°C/hour & 80°- 120°C/hour |  |  |  |  |  |  |

| Technique Details : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Method of Back Gouging and Cleaning Brushing & Grinding |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| String or Weave bead |  |  | : |  | Both |  |  |  |  |  |  |  | Weaving (maximum width of run) 3 x Elct Core Dia |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Amplitude |  |  | : |  | N/A | Frequency |  |  | : | N/A |  |  |  |
| Welding Details |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Run | Process | Weld |  | Electrodes Spec Class |  |  |  | Size of Filler Metal (mm) |  |  | Current Range (Amp) |  |  | Voltage Range (Volt) | Type of Current/ Polarity |  |  | Wire Feed Speed (mm/min) | Travel Speed Range (mm/min) | Heat Input (Kj/mm) Max |
| 1 | SMAW | Root Pass |  | A5.1 |  | E6013 |  | 3.2 |  |  | 85 ± 10% |  |  | 27 ± 7% | DC+ |  |  | - | 80 ± 10% | 3.5 |
| 2 | SMAW | Hot Pass |  | A5.1 |  | E6013 |  | 3.2 |  |  | 100 ± 10% |  |  | 27 ± 7% | DC+ |  |  | - | 90 ± 10% | 3.5 |
| 3 | SMAW | Filler Pass |  | A5.1 |  | E6013 |  | 3.2 |  |  | 150 ± 10% |  |  | 27 ± 7% | DC+ |  |  | - | 130 ± 10% | 3.5 |
| 4 | SMAW | Filler Pass |  | A5.1 |  | E6013 |  | 3.2 |  |  | 150 ± 10% |  |  | 27 ± 7% | DC+ |  |  | - | 130 ± 10% | 3.5 |
| 5 | SMAW | Capping |  | A5.1 |  | E6013 |  | 3.2 |  |  | 140 ± 10% |  |  | 27 ±7% | DC+ |  |  | - | 120 ± 10% | 3.5 |
| BACKSIDE TREATMENT : CARBON ARC GOUGING |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6 | SMAW | Fill / Cap |  | A5.1 |  | E6013 |  |  | 3.2 |  | 140 ± 10% |  |  | 27 ±7% | DC+ |  |  | - | 120 ± 10% | 3.5 |

Other Information

| Manufacture PT.Bumi Laut Perkasa | Surveyor to Bureau Veritas Office |
| --- | --- |
| Date : Name : Signature : | Date : Name : Signature : |